# CD - Compact Disc

CDs and DVDs are everywhere these days. Whether they are used to hold music, data or computer software, they have become the standard medium for distributing large quantities of information in a reliable package. Compact discs are so easy and cheap to produce that America Online sends out millions of them every year to entice new users. And if you have a computer and CD-R drive, you can create your own CDs, including any information you want.

### Material

The usual CD can store up to 74 minutes of music, so the total amount of digital data that must be stored on a CD is 783,216,000 bytes. To fit more than 783 megabytes (MB) onto a disc only 4.8 inches (12 cm) in diameter requires that the individual bytes be very small. By examining the physical construction of a CD, you can begin to understand just how small these bytes are.

A CD is a fairly simple piece of plastic, about 1.2 mm thick. Most of a CD consists of an injection-moulded piece of clear polycarbonate plastic. During manufacturing, this plastic is impressed with microscopic bumps arranged as a single, continuous, extremely long spiral track of data. Once the clear piece of polycarbonate is formed, a thin, reflective aluminium layer is sputtered onto the disc, covering the bumps. Then a thin acrylic layer is sprayed over the aluminium to protect it. The label is then printed onto the acrylic.

### The Spiral

A CD has a single spiral track of data, circling from the inside of the disc to the outside. The fact that the spiral track starts at the centre means that the CD can be smaller than 4.8 inches (12 cm) if desired, and in fact there are now plastic baseball cards and business cards that you can put in a CD player. CD business cards hold about 2 MB of data before the size and shape of the card cuts off the spiral.

### Bumps

The elongated bumps that make up the track are each 0.5 microns wide, a minimum of 0.83 microns long and 125 nanometers high. (A nanometer is a billionth of a meter.)

You will often read about "pits" on a CD instead of bumps. They appear as pits on the aluminum side, but on the side the laser reads from, they are bumps.

The incredibly small dimensions of the bumps make the spiral track on a CD extremely long. If you could lift the data track off a CD and stretch it out into a straight line, it would be 0.5 microns wide and almost 5 km long! To read something this small you need an incredibly precise disc-reading mechanism.